## Slide 1: MFM Capacitor
Dutta Lab

## Slide 2
Stress Voltage 2V
Stress Voltage 2.5V
Stress Voltage 3V
Endurance Test at H0.5Z0.5O with 1μs PW and 100ns Trise/fall
After Fine Tuning in cycles

## Slide 3
Endurance Test at H0.5Z0.5O with 1μs PW and 100ns Trise/fall
Random
Median
After Fine Tuning in cycles
Random stress voltage

## Slide 4
log(CBD)=-5.76v+16.62
SSE | 0.6535
R-square | 0.9695
DFE | 7
Adj R-sq | 0.9651
RMSE | 0.3056
Fitting Data with Random Stress Voltage

## Slide 5
log(CBD)=-5.46v+18.9
SSE | 0.7049
R-square | 0.9845
DFE | 7
Adj R-sq | 0.9822
RMSE | 0.3173
Fitting Data with Uniform Stress Voltage

## Slide 6
E (MV/cm)
1/CBD
log(1/CBD) = 3.2736*E - 18.9037
Fitting Data with Uniform Stress Voltage

## Slide 7
E (MV/cm)
1/CBD
log(1/CBD) = 3.4537*E - 19.6168
Fitting Data with Random Stress Voltage

## Slide 8
Literature Summary
Failure Rate,
Ref: Ravikumar, Priyanka G. “Comprehensive time dependent dielectric breakdown (TDDB) characterization of ferroelectric capacitors under bipolar stress conditions”. 2024 IEEE International Reliability Physics Symposium (IRPS)

## Slide 9: 1st Experiment
Stress Voltage (v) | 2.5 | 2.8 | 3.1 | 2.95 | 2.3 | 2.65 | 2.65
Cycles to Breakdown (Cbd) | 3.00E+05 | 3000 | 100 | 700 | 5.00E+06 | 1.00E+04 | 3.00E+04
Initialize Data

## Slide 10
3V
n=123.9849, b=0.9256
2.6V
n=5129.3206, b=1.2741
2.2V
n=2677654.3546, b=1.1837
Weibull Distribution
Failure Rate,
ln(-ln(1-F)) = 1.1837 ln(CBD) - 17.5187
ln(-ln(1-F)) = 1.2741 ln(CBD) - 10.8843
ln(-ln(1-F)) = 0.9256 ln(CBD) - 4.4615
ln(CBD)

## Slide 11
3V
2.6V
2.2V
85˚C
Endurance @ 850C
log(1/CBD) = 3.2897*E -18.1335

## Slide 12
log(1/CBD) = 3*E - 19.9
Endurance @ 850C